| SÄKAPHEN GmbH Bottroper Str. 275 D – 45964 Gladbeck Tel.: +49(0)2043/947-0 Fax: +49(0)2043/947-130 E-Mail: info@saekaphen.de | TECHNICAL DOCUMENTATION |  |
| --- | --- | --- |
| SÄKAPHEN Coating Säka-Flake 900 Product Data Sheet Basis: Vinylester resin, catalytic hardening Product description: Säka-Flake 900 beige is a coating which is based on vinylester resin, and is filled with inert mineral flakes. It distinguishes itself by high temperature resistance and excellent resistance properties to aggressive agents as acids, bases, solvents, salt solvents, fluegas and all different kind of waters. By these properties Säka-Flake 900 is a coating system with excellent chemical resistance and long protection against corrosion, especially in the high temperature range. Temperature resistance: up to 220°C dry humid / wet depending on the agent Field of application: Coating of fluegas funnels/channels, fluegas desulfurization parts, wash towers, process tanks, storage tanks, vessels and containers. Application method: to be applied by rolling, brushing, spraying or airless spraying. Number of the spraying process: 2 - 4 layers approx., 0,4 – 0,5 mm per layer Total dry film thickness: 0,8 – 2,5 mm depending on the medium used Drying between the working operations (coatings): At least ten hours, however, no longer than three days. Mixing ratio: Comp. A Part weight: 100 Comp. B (hardener) Part weight: 4 |  |  |

| SÄKAPHEN GmbH Bottroper Str. 275 D – 45964 Gladbeck Tel.: +49(0)2043/947-0 Fax: +49(0)2043/947-130 E-Mail: info@saekaphen.de | TECHNICAL DOCUMENTATION |  |
| --- | --- | --- |
| - - 2 - Pot life: at 15°C: 120 min at 20°C: 90 min at 30°C: 50 min Technical data: Technical data; Value; unit; standards. Colour; beige. Density; 1,28; g/cm³; DIN EN ISO2811-1. Viscosity; 5000; mPa.s; DIN 53299. Hardness; 87; Shore D; DIN 53505. Tensile strength; 12; M Pa; EN ISO 527. Elongation; 1,5; %; EN ISO 527. Water absorption; < 1,0; %; DIN EN ISO 62. |
| On condition that storing is made dry and cool, the product durability is nine months. Theoretical consumption: 1,6 kg/m² at 1000 µm dry film thickness (DFT) Safety measures: All data relevant for safety are specified in the EG-Safety Data Sheets. - This technical information is in correspondence with the latest development in research and product knowledge, and has to be understood as general information only. |  |  |