Table of contents

Chapter V

5. 	Processing guidelines and product data sheets

5.1 	Thermally hardening SÄKAPHEN coatings

- Si 14 E

- Si 14 EG

- Si 17 E

- Si 57 E

- Si 57 EN

- Si 57 EG

5.2 	Catalytically hardening SÄKAPHEN-coatings

- HR 60 extra G

- HR 60 extra TG

- SÄKA-FLAKE 1042/1042S

- SÄKALINE SG

5.3	Instruction for repair   RE

-HR 60 extra RE

-SÄKA-FLAKE 1042/1042S RE

5.1 	Processing guidelines for thermally hardening materials

SÄKAPHEN coating

Si 14E

Construction notes

All welding seams must be smooth and free from welding splashes. Undercuts and sharp edges must be ground down. Other rules in accordance with DIN 28051 and DIN 28053.

Surface preparation

Blast cleaning is necessary to achieve a white-metallic surface in accordance with purity grade SA3 and a roughness depth of 40 - 60µm (in accordance with Swedish Standard 055900 or DIN 4768).

Quantities

Theoretical quantities

1.2 kg/m² 		Si 14E

Dry film coating thickness

approx 200 µm 	Si 14E when spraying

approx 200 µm 	Si 14E when flooding

Dilution

The quantity of diluter depends on the temperature, ventilation, air humidity and spraying equipment in use, taking into account the given layer thickness.

Recommended addition of dilution at 20° C is approx. 20 - 30 %. We recommend the following mixtures:

Ethyl alcohol 	50 %

n-Butanol 		48 %  -  46 %

IPA 		 2 %  -    4 %

Mixing

The correct viscosity is achieved by careful and thorough mixing according to our recommendations.

Spraying application 	Viscosity (flow time) according to DIN 53211 (DIN cup 4) for a spraying nozzle size of 0.5 to 1.5 mm.

50 to 80 seconds

Flooding application 	       40 to 80 seconds

Intermediate baking 	Reaching a temperature of 90° C within 120 min. with a holding time of 60 min. Then a further rise of temperature, up to 120/130° C within 30 min. with a holding time of 30 min. Intermediate baking is terminated as soon as all solvent smells have disappeared.

After intermediate baking and cooling to standard temperature the coating must be dissolvable with acetone.

Final baking 	Reaching a temperature of 110° C within 90 min. with a holding time of 30 min. Then a further rise of temperature, up to 200/210° within 120 min. with a holding time of 60 min. The temperature measuring instrument indicates the end of the baking process. The coating may not be dissolvable with acetone any more after cooling to standard temperature and color dissolution must not occur when the coating is rubbed with a clean test cloth.

Coating 		1.	The coating material is to be processed with clean 					and functional equipment.

2.	The air supply should be free from foreign matter. 					The operating pressure must be adjusted to 4 -6 bar 					or approx. 3 bar in the pressure tank. Any spraying 					gun with a nozzle of size 0.5 to 1.5 mm can be used.

3.	Spraying of 3 – 4 cross layers to build up wet 	layer.

4.	Air-drying of the object during a period of 60 - 90 min. 					with appropriate ventilation, as preparation for 						baking.

5.	After air-drying, combustion begins as described 					under intermediate baking.

6.	The dry film coating thickness should be measured 					after 3–4 layers. Repetition of the measurement after 					each layer.

7.	When a dry film coating thickness of approximately 					180-200µm is reached, a  preliminary test 						(intermediate test) before the final baking is carried 					out with a test voltage of 800 V. The coating must be 					absolutely nonporous. If it is not, a further layer must 					be applied and another preliminary test must be 					performed.

Equipment for

Coating		1.	Normal spraying equipment for a pressure between

4 - 6 bar or approx. 3 bar in the pressure tank or 					spraying guns with nozzles of size of 0.5 to 1.5 mm.

2.	Brushes and paint-brushes

3.	DIN cup 4 for determination of the flow time 				  		(viscosity) in accordance with DIN 53211.

4.	Sandblasting lances, especially for heat 						exchanger-pipes using e.g. slag blast grain with a 					grain size of 0.7-1.4 mm.

5.	Layer thickness measuring instrument:							Minitest 4.100 of 0 - 3.000 µm

6.	Pore detecting device Porotest 7

operating range 0.5 - 7.0 kV.

Storage rules 		The steel drums must be sealed and stored in a cool and dry Area, at a standard temperature of 10 - 15° C.				and a relative humidity of approx. 50-60 %. Then the 				durability amounts to approx. 24 months after delivery.

Durability after

opening	After opening and resealing the steel drums after using parts of the material, the durability of the remaining material is approx. 6 months within the above mentioned 24 months. The already diluted material can be stored at a standard temperature of 10 - 15° C and a relative humidity of approx. 50-60 % for approx. 3 months, if it is well sealed.

SÄKAPHEN Coating

Si 14 E

Product Data Sheet

Characteristics:			duroplast coating

Basis:					phenolic resin combination

Colour:				green / brilliant

Fields of Application:			heat exchangers, air coolers, condensers, 								evaporators, turbine and compressor rotors, 								salt dissolving installations, pipework,centrifuges,tank cars

Chemical Resistance:	resistant to acids, salt solutions, cooling waters,

gases, organic solvents

Film Thickness:			approx. 200 µm

Temperature Resistance:		- 70° C to + 180° C

Heat conductivity:			2,65 W/mK

pH-Range:				1 to 8

Pinhole Testing:			800 Volt DC

Pendulum Hardness acc.

to König:				182 sec.

Break-off Resistance:			15 N/mm²

ASTM D 4541

Impact Strength:			560 mm fall / 1 kg

acc. to DIN 55669

SÄKAPHEN coating

Si 14EG

Construction notes

All welding seams must be smooth and free from welding splashes. Undercuts and sharp edges must be ground down. Other rules in accordance with DIN 28051 and DIN 28053.

Surface preparation

Jet cleaning is necessary to achieve a white-metallic surface in accordance with purity grade SA3 and a roughness depth of 40 - 60µm (in accordance with Swedish Standard 055900 DIN 4768).

Quantities

Theoretical quantities

1.2 kg/m² 		Si 14EG

Dry film coating thickness

approx 250 µm 	Si 14EG when spraying

approx 250 µm 	Si 14EG when flooding

Dilution

The quantity of the diluter depends on the temperature, ventilation, air humidity and spraying equipment in use, taking into account the given layer thickness.

Recommended addition of dilution at 20° C is approx. 10 - 20 %. We recommend the following mixtures:

Ethyl alcohol 	50 %

n-Butanol 		48 %  -   46 %

IPA 		 2 %  -     4 %

Mixing

The viscosity is achieved by careful and thorough mixing in accordance with our recommendations.

Spraying application	Viscosity (flow time) according to DIN 53211 DIN cup 4 for a spraying nozzle size of 0.5 to 1.5mm.

50 to 80 seconds

Flooding application 		40 to 80 seconds

Intermediate baking 	Reaching a temperature of 90° C within 120 min. with a 	holding time of 60 min. Then a further rise of 	temperature up to 120/130° C within 30 min. with a 	holding time of 30 min. Intermediate baking is terminated 	as 	soon as no more solvent smell arises. After 	intermediate baking and cooling to standard temperature the 	coating must be dissolvable with acetone.

Final baking 	Reaching a temperature of 110° C within 90 min. with a 	holding time of 30 min. Afterwards a further rise of the tem-	perature up to 200/210° within 120 min. with a holding time of 60 	min.The temperature measuring instrument indicates the end of 	the baking process. The coating may not be dissolvable with 	acetone any more after cooling to standard temperature, and no 	color dissolution must be visible on a clean test cloth.

Coating 	1.	The coating material is to be processed with 				clean, common spraying equipment.

2. 	The air supply should be free from foreign 				matter. Adjustment of the operating 					pressure: to 4-6 bar or approx. 3 bar 					in tank. Any spraying gun with nozzle size 				0.5 to 1.5 mm can be used.

3.	Spraying of 3-4 cross layers to build the wet layer.

4.	Air-drying the object during a period of 60 - 90 min. 			with appropriate ventilation as preparation for baking.

5. 	After air-drying the combustion begins as described 			under  intermediate baking.

6. 	The dry film coating thickness should be measured 			after 3-4 layers. Then repetition of the measurement 			after each layer.

7.	If a dry film coating thickness of approximately 250 			µm is reached, a preliminary test (intermediate test) 			before the final baking is performed at a test 				voltage of 800 V. The coating must be absolutely 			nonporous. If it is not, a further layer must be applied 			and another preliminary test must be performed.

Equipment for

Coating	1. 	Normal spraying equipment for a pressure 				between 4-6 bar or approx. 3 bar in the pressure 			tank, or spraying guns with nozzle sizes

of 2.5 to 3.0 mm.

2. 	Brushes and paint-brushes.

3.	DIN cup 4 for determination of the flow time 					(viscosity) in accordance with DIN 53211.

4.  Sandblasting lances, especially for heat exchanger pipes

using e.g. slag blast grain with a grain size of 0.7 - 1.4 mm.

5.   Layer thickness measuring instrument:Minitest

4.100 from 0 - 3.000 µm.

6.	Pore detecting device Porotest 7					              	operating range 0.5 - 7.0 kV.

Storage rules	The Steel drums must be sealed and stored in a cool and dry area at standard temperature of 10 - 15° C and a relative humidity of approx. 50 - 60 %. The durability amounts then to approx. 24 months after delivery.

Durability after

Opening	After opening and resealing the Steel drums after using parts of the material the durability of the remaining material is approx. 6 months within the above mentioned 24 months. The already diluted material can be stored at standard temperature of 10 - 15° C and relative humidity of approx. 50 - 60 %. for approx. 3 months if it is well sealed.

SÄKAPHEN Coating

Si 14 EG

Product Data Sheet

Characteristics:			duroplast coating

Basis:					phenolic resin combination

Colour:				brownred / mat

Fields of Application: 	condensers, condensate receivers, degassers, hot water and steam stressed paint parts

Chemical Resistance:	diffusion resistant in weak acid to light alkaline aqueous liquids and vapours

Film Thickness:			approx. 250 µm

Temperature Resistance:		- 70° C to + 180° C

Heat conductivity:			3,46 W/mK

pH-Range:				3 to 8

Pinhole Testing:			800 Volt DC

Pendulum Hardness acc.

to König:				134 sec.

Break-off Resistance:			6 N/mm²

ASTM D 4541

Impact Strength:			470 mm fall / 1 kg

acc. to DIN 55669

SÄKAPHEN coating

Si 17E

Construction notes

All welding seams must be smooth and free from welding splashes. Undercuts and sharp edges must be ground down. More rules in accordance with DIN 28051 and DIN 28053.

Surface preparation

Blast cleaning is necessary to achieve a white-metallic surface of purity grade SA3 and a roughness depth of 40 - 60µm (in accordance with Swedish standard 055900 or DIN 4768).

Quantities

Theoretical quantities

0,8 kg/m² 		Si 17E

Dry film coating thickness

approx 180 µm 	Si 17E when spraying

Dilution

The quantity of the diluter depends on the temperature, ventilation, air humidity and spraying equipment in use, taking into account the given layer thickness.

Recommended addition of dilution with 20° C is approx. 20 - 30 %. We recommend the following mixtures:

Ethyl alcohol 	50 %

n-Butanol 		48 %   -  46 %

IPA 		 2 %  -     4 %

Mixing

The correct viscosity is achieved by careful and thorough mixing in accordance with our recommendations.

Spraying application 	Viscosity (flow time) according to DIN of 53211 DIN cup 4 for a spraying nozzle size of 0.5 to 1.5mm

50 to 80 seconds

Intermediate baking 	Reaching a temperature of 70° C within 60 min. with a 	holding time of 60 min. Afterwards a further rise of 	temperature 	up to 120/130° C within 30 min. with a holding time of 90 min. 	The intermediate baking is 	terminated as soon as no 	more solvent smell arises. After the intermediate baking and 	cooling to standard temperature the coating must be 	dissolvable with acetone.

Final baking 	Reaching a temperature of 70° C within 60 min. with a 	holding time of 60 min. Afterwards a further rise of the 	temperature up to 120/130° within 30 min. with a holding time 	of 30 min., and another rise up to 210° C within 90 min. with a 	holding time of 90 min.The temperature measuring instrument 	indicates the end of the baking process.

The coating must not be dissolvable any more with 	acetone 	after cooling to standard temperature and color dissolution 	on 	a clean test cloth must not occur.

Coating 			1.	The coating material is to be processed with 						clean, common spraying equipment.

2. 	The air supply should be free from foreign 						matter. The operating pressure has to be 						adjusted to 4-6 bar or approx. 3 bar in the 						pressure tank. Any spraying gun with nozzle 						sizes of 0.5 to 1.5 mm can be used.

3. 	Spraying of 3-4 cross layers to build up the wet 						layer.

4. 	Air-drying the object for 60 - 90 min., with 								appropriate ventilation as preparation for 								baking.

5. 	After air-drying the combustion begins, as 						described under intermediate baking.

6. 	The dry film coating thickness should be 						measured after 3 - 4 layers. Repetition of the 						measurement after each baked layer.

7. 	When a dry film coating thickness of 							approximately 180 µm is reached, a preliminary 					test (intermediate test) before the terminal 						baking with the wet-test equipment is 							performed with a testing voltage of 9 V. 							The coating must be absolutely nonporous. If it 						is not, a further layer must be applied and 						another preliminary test must be performed.

Equipment

for coating			1. 	Normal spraying equipment for a pressure 				between 4 - 6 bar or approx. 3 bar in the 				pressure tank, or spraying guns with nozzle 				sizes of 0.5 to 1.5 mm.

2. 	Brushes and paint-brushes.

3.	DIN cup 4 for determination of the flow time 						(viscosity) in accordance with DIN 53211.

4. 	Layer thickness measuring instrument: Minitest 	4.100 	from 0 - 3.000 µm

5. 	Pore detecting device wet-tester “Elcometer 270”

test voltage of 67,5 Volt.

Storage rules 	The Steel drums must be sealed and stored in a cool and dry area at standard temperature of 10 - 15° C and at relative humidity of approx. 50 - 60 %. The durability is then approx. 24 months after delivery.

Durability after

opening	When opening and resealing the Steel drums after using 	parts of the material, the durability is approx. 6 months 	within the above mentioned 24 months. The already 		diluted material can be stored at standard temperature of

10 - 15° C and a relative humidity for approx. 3 months, if it is 	well sealed.

SÄKAPHEN Coating

Si 17 E

Product Data Sheet

derivation ability for electrostatic charges

Characteristics:			duroplast coating

Basis:					phenolic resin combination

Colour:				olive / halfmat

Fields of Application:	Linings of steel containers for the storage of inflammable liquids

classified as dangerous according to class AI / AII and B as well as for water endangering non-in-flammable liquids (alphatic chlorinated hydrocarbons)

Chemical Resistance:	liquid and gaseous hydrocarbons, salt solutions, oils and greases; acid to weak alkaline liquids

up to max. 8 pH-range

Film Thickness:			approx. 180 µm

Pinhole Testing:			67,5 Volt wet sponge test

Temperature Resistance:		- 70º C to + 180º C

Heat conductivity:			9,24 W/mK

pH Range:				2 – 8

Pendulum Hardness acc.

to König:				148 sec.

Break-off Resistance:			25,0 N/mm²

DIN ISO 4624

Impact Strength:			1.000 mm fall / 430 g

acc. to DIN 55669

Specific Resistance:			considerably below 107 Ohm

BGR 132

SÄKAPHEN coating

Si 57E

Construction notes

All welding seams must be smooth and free from welding splashes. Undercuts and sharp edges must be ground down. Other rules in accordance with DIN 28051 and DIN 28053.

Surface preparation

Jet cleaning is necessary to achieve a white-metallic surface of purity grade SA 3 and a roughness depth of 40 - 60µm (in accordance with Swedish standard 055900 or DIN 4768).

Quantities

Theoretical quantities

0.6 kg/m² 			Si 57E priming coat

0.5 kg/m² 			Si 57E

Dry film coating thickness

when spraying:

100 µm 			Si 57E priming coat

approx. 80 -100 µm 		Si 57E

when flooding:

approx. 100 µm 		Si 57E priming coat

approx. 80 – 120µm 		Si 57E

Dilution

The quantity of diluter depends on the temperature, ventilation, the air humidity and the used spraying equipment, taking into account the given layer thickness.

Recommended addition of diluter at 20° C approx. 10 - 20 %. We recommend the following application:

1 % parts of weight n-Butanol and

2 % parts of weight Toluene

Mixing

The correct viscosity is achieved by careful and thorough mixing in accordance with our recommendations.

Spraying application:

Viscosity (flow time) according to DIN 53211 (DIN cup 4)  for a spraying nozzle size of 0.5 to 1.5 mm

50 - 80 seconds 		SI 57E priming coat

50 - 80 seconds 		SI 57 E

Flood application: 	40 - 80 seconds 		SI 57E priming coat

40 - 80 seconds		SI 57E

Intermediate baking 		Reaching a temperature of 90° C within of 60 min. 		with a holding time of 30 min. Then a further rise of 		the temperature up to 130° C within 30 min. with a 		holding time of 30 min. Then the temperature 		must be increased to 150° C in 30 min. with a 		holding time of 90 min. The intermediate baking 		process is terminated as soon as no more solvent 		smell arises. After intermediate baking and cooling 		to standard temperature the coating must be 		dissolvable with acetone.

Final baking 	Reaching a temperature of 90° C within 60 min. 	with a holding time of 30 min. Then a further rise of 	the temperature to 130° C within 30 min. with a 	holding time of 30 min. Then the temperature must 	be increased to 150° C within 30 min. with a 	holding time of 30 min. The temperature has then 	to be increased to 210° C in 90 min. with a holding 	time of 30 min.

The coating may not be dissolvable any more with 	acetone after cooling to standard temperature and 	color dissolution must not be visible on a clean test 	cloth.

Coating 	1. 	The coating material has to be processed with 		clean, common spraying equipment.

2. 	The air supply should be free from foreign 		matter. The operating pressure must be 		adjusted to 4 -6 bar or approx. 3 bar in the 		pressure tank. Any spray gun with nozzle sizes 		of 0.5 to 1.5mm can be 	used.

3. 	Spraying of 3-4 cross layers to build the wet layer.

4. 	Air-drying the object for 60 - 90 min. 					with appropriate ventilation as preparation for 				baking.

5. 	After air-drying the combustion begins, as 				described under intermediate baking.

6. 	The dry film coating thickness should be 				measured after 3 - 4 layers. Repetition of the 				measurement after each baked layer.

7. 	When a dry film coating thickness of 					approximately 180 µm is reached, a preliminary 				test (intermediate test) before final baking is 				performed with the wet-test equipment at a test 				voltage of 800V. The coating must be 					absolutely nonporous. If it is not, a further layer 				must be applied and another preliminary test 				must be performed.

Equipment for

coating 		1. 	Normal spraying equipment for a pressure between 4 - 6 bar

or approx. 3 bar in the pressure tank, or 			spraying guns of nozzle size of 0.5 to 1.5 mm.

2. 	Brushes and paint-brushes.

3.	DIN cup 4 for determination of the flow time 				(viscosity) in accordance with DIN 53211.

4.  Sand blasting lances, especially for

heatexchanger pipes using e.g. slag blast grain

with a grain size of 0.7 - 1.4 mm.

5.   Layer thickness measuring instrument:

Minitest 4.100 from 0 - 3.000 µm

6. 	Pore detecting device Porotest 7

operating range 0.5 - 7.0 kV.

Storage regulations		The Steel drums must be sealed and stored in a cool and dry area at standard temperature of 10 - 15° C and 	relative humidity of approx. 50 - 60 %. The durability amounts then to approx. 24 months after delivery.

Durability after

Opening	After opening and resealing the Steel drums after using parts of the material, the durability is approx. 6 months within the above mentioned 24 months. The already diluted material can be stored at standard temperature of 10 - 15° C and at relative humidity of 50-60 % for approx. 3 months, if it is well sealed.

SÄKAPHEN Coating

Si 57 E

Product Data Sheet

Characteristics:			duroplast coating

Basis:					phenolic epoxy resin

Colour:				oxide red / brilliant

Fields of Application:		heat exchangers, condensers, evaporators, water treatment      	equipment, desalization plants for sea water, pipework of 	steel and stainless steel

Chemical Resistance:		resistant to strong alkaline to weak acid media, all type of 	cooling waters including brackish-, river- and sea-water, salt 	solutions, greases, oils solvents, gases, food, physiological 	harmless

Film Thickness:			approx. 180 µm

Temperature Resistance:		- 100° C to + 180 ºC

Heat conductivity			2,51 W/mK

pH-Range:				3 to 14

Pinhole Testing:			800 Volt DC

Pendulum Hardness acc.

to König:				200 sec.

Break-off Resistance:			15 N/mm²

ASTM D 4541

Impact Strength:			> 1000 mm fall / 1 kg

acc. to DIN 55669

SÄKAPHEN coating

Si 57EN

Construction notes

All welding seams must be smooth and free from welding splashes. Undercuts and sharp edges must be ground down. Other rules in accordance with DIN 28051 and DIN 28053.

Surface preparation

Jet cleaning is necessary to achieve a white-metallic surface of purity grade SA 3 and a roughness depth of 40 - 60µm (in accordance with Swedish standard 055900 or DIN 4768).

Quantities

Theoretical quantities

1.2 kg/m² 			Si 57EN

Dry film coating thickness

when spraying:

approx 200 µm 		Si 57EN

when flooding:

approx 200µm 		Si 57EN

Dilution

The quantity of diluter depends on the temperature, ventilation, the air humidity and the used spraying equipment, taking into account the given layer thickness.

Recommended addition of diluter at 20° C approx. 10 - 20 %. We recommend the following application:

1 % parts of weight n-Butanol and

2 % parts of weight Toluene

Mixing

The correct viscosity is achieved by careful and thorough mixing in accordance with our recommendations.

Spraying application:

Viscosity (flow time) according to DIN 53211 (DIN cup 4)  for a spraying nozzle size of 0.5 to 1.5 mm

50 - 80 seconds

Flood application: 	40 – 80 seconds

Intermediate baking 		Reaching a temperature of 90° C within of 60 min. with a 				holding time of 30 min. Then a further rise of the

temperature up to 130° C within 30 min. with a holding 					time of 30 min. Then the temperature must be increased 				to 150° C in 30 min. with a holding time of 90 min. The 					intermediate baking process is terminated as soon as no 				more solvent smell arises. After intermediate baking and 				cooling to standard temperature the coating must be 					dissolvable with acetone.

Final baking 		Reaching a temperature of 90° C within 60 min. with a 			holding time of 30 min. Then a further rise of the 			temperature to 130° C within 30 min. with a holding time of 		30 min. Then the temperature must be increased to 			150° C within 30 min. with a holding time of 30 				min. The temperature has then to be increased to 			210° C in 90 min. with a holding time of 	30 min. The coating 		may not be dissolvable any more with acetone after 			cooling to standard temperature and color dissolution 			must not be visible on a clean test cloth.

Coating 	1. 	The coating material has to be processed with clean, 			common spraying equipment.

2. 	The air supply should be free from foreign matter. 			The operating pressure must be adjusted to				4 -6 bar or approx. 3 bar in the pressure tank. Any 			spray gun with nozzle sizes of 0.5 to 1.5mm can be 			used.

3. 	Spraying of 3-4 cross layers to build the wet layer.

4. 	Air-drying the object for 60 - 90 min. 							with appropriate ventilation as preparation for baking.

5. 	After air-drying the combustion begins, as described 					under intermediate baking.

6. 	The dry film coating thickness should be measured 					after 3 - 4 layers. Repetition of the measurement 					after each baked layer.

7. 	When a dry film coating thickness of approximately 					180 µm is reached, a preliminary test (intermediate 					test) before final baking is performed with the wet-					test equipment Porotest1 at a test voltage of 9V.

The coating must be absolutely nonporous. If it is 					not, a further layer must be applied and another 					preliminary test must be performed.

Equipment for

coating 		1. 	Normal spraying equipment for a pressure between

4 - 6 bar or approx. 3 bar in the pressure tank, or 			spraying guns of nozzle size of 0.5 to 1.5 mm.

2. 	Brushes and paint-brushes.

3.	DIN cup 4 for determination of the flow time 		(viscosity) in accordance with DIN 53211.

4.   Sand blasting lances, especially for heat exchanger pipes using e.g. slag blast grain with a grain size of 0.7 - 1.4 mm.

5. 	Layer thickness measuring instrument:

Minitest 4.100 from 0 - 3.000 µm

6. 	Pore detecting device wet-tester “Elcometer 270”

Test voltage of 67,5 Volt.

Storage regulations		The Steel drums must be sealed and stored in a cool and dry area at standard temperature of 10 - 15° C and relative humidity of approx. 50 - 60 %. The durability amounts then to approx. 24 months after delivery.

Durability after

Opening	After opening and resealing the Steel drums after using parts of the material, the durability is approx. 6 months within the above mentioned 24 months. The already diluted material can be stored at standard temperature of 10 - 15° C and at relative humidity of 50-60 % for approx. 3 months, if it is well sealed.

SÄKAPHEN Coating

Si 57 EN

Product Data Sheet

Characteristics:			duroplast coating with improved heat conductivity

Basis:					phenolic epoxy resin

Colour:				oxide red / brilliant

Fields of Application:		heat exchangers, condensers, evaporators, water treatment 	equipment, desalization plants for sea water, pipework of 	steel and stainless steel

Chemical Resistance:		resistant to strong alkaline to weak acid media, all type of 	cooling waters including brackish-, river- and sea-water, salt 	solutions, greases, oils solvents, gases, food, physiological 	harmless

Film Thickness:			approx. 180 µm

Temperature Resistance:		- 100° C to + 180 ºC

Heat conductivity:			3,53 W/mK

pH-Range:				3 to 14

Pinhole Testing:			67,5 Volt wet test

Pendulum Hardness acc.

to König:				200 sec.

Break-off Resistance:			15 N/mm²

ASTM D 4541

Impact Strength:			> 1000 mm fall / 1 kg

acc. to DIN 55669

SÄKAPHEN coating

Si 57EG

Construction notes

All welding seams must be smooth and free from welding splashes. Undercuts and sharp edges must be ground down. More rules in accordance with DIN 28051 and DIN 28053.

Surface preparation

Jet cleaning is necessary to achieve a white-metallic surface of purity grade SA 3 and a roughness depth of 40 - 60µm (in accordance with Swedish Standard 055900 or  DIN 4768).

Quantities

Theoretical quantities

1.3 kg/m² 	Si 57EG

Dry film coating thickness when spraying:

approx 250 µm 	Si 57EG

When flooding:

approx 250 µm 	Si 57EG

Dilution

The quantity of the diluter depends on the temperature, ventilation, air humidity and spraying equipment in use, taking into account the given layer thickness.

Recommended addition of diluter at 20° C: approx. 10 - 20 %. We recommend the following mixture:

1 % parts by weight n-Butanol and

2 % parts by weight Toluene

Mixing

The correct viscosity is achieved by careful and thorough mixing in accordance with our recommendations.

Spraying application		Viscosity (flow time) according to DIN 53211 DIN cup 4 for a spraying nozzle size of 0.5 mm to 1.5 mm

50 to 80 seconds

Flood application 	40 to 80 seconds

Intermediate baking 	Reaching a temperature of 90° C within 60 min. with a holding time of 30 min. Then a further rise of the temperature up to 130° C within 30min. with a holding time of 30 min. Then the temperature is to be increased to 150° C in 30 min. with a holding time of 90 min.Intermediate baking is terminated as soon as that no more solvent smell arises. After intermediate baking and cooling to standard temperature, the coating must be 	dissolvable with acetone.

Final baking 	Reaching a temperature of 90° C within 60 min. with a 	holding time of 30min.Then a further rise of 	temperature up to 130° within 30min. with a holding time of 	30 min. After that, the temperature has to be increase to 	150°C with in 30 min. with a holding time of 90 min. The 	temperature is then increased to 210° C in 90 min. with a 	holding time of 30 min.

The coating must not be dissolvable with acetone any 	more after cooling to standard temperature, and color 	dissolution may not be visible on a clean test cloth.

Coating 	1.	The coating material is to be processed with clean, 			common spraying equipment.

2. 	The air supply should be free from foreign matter. 					The operating pressure has to be adjusted to 						4-6 bar or approx. 3 bar in the pressure tank. Any 					spraying gun with nozzle size 0.5 to 1.5 mm can 					be used.

3. 	Spraying of 3-4 cross layers to build up the wet layer.

4.	Air-drying the object for 60 - 90 min. 							with appropriate ventilation as preparation for baking.

5. 	After air-drying the combustion begins as described 					under intermediate baking.

6. 	The dry film coating thickness should be measured 					after 3-4 layers. Then repetition of the measurement 					after each layer.

7.	When a dry film coating thickness of approximately 					250 µm is reached, a preliminary test (intermediate 					test) is performed before final baking, using a testing 					voltage of 800 V. The coating must be absolutely 					nonporous. If it is not, a further layer must be applied 					and another preliminary test must be performed.

Equipment for

coating 	1. 	Normal spraying equipment for a pressure between 			4-6 bar or approx. 3 bar in the pressure tank or 				spraying guns with nozzle size 2.5 to 3.0 mm.

2. 	Brushes and paint-brushes.

3.	DIN cup 4 for determination of the flow time 						(viscosity) in accordance with DIN 53211.

4.	Sandblastinglances, especially for heat exchanger pipes

using e.g. slag blast grain with a grain size of 0.7 - 1.4 mm.

5.   Layer thickness measuring instrument:

Minitest 4.100 from 0 - 3.000 µm

6.	 Pore detecting device Porotest 7

operation range 0.5 - 7.0 kV.

Storage regulations 		The Steel drumsmust be sealed and stored in a cool and dry area at standard temperature of 10 - 15° C and relative humidity of approx. 50 - 60 %. The durability is then approx. 24 months after delivery

Durability after

opening	After opening and resealing the Steel drums after using parts 	of the material, the durability is to approx. 6 months within 	the 	above mentioned 24 months. Already diluted material can be 	stored at standard temperature of 10 - 15° 	C and at a relative

humidity of 50-60 % for approx. 3 	months, if it is well sealed

SÄKAPHEN Coating

Si 57 EG

Product Data Sheet

Characteristics:			duroplast coating with improved heat conductivity

Basis: 					phenolic epoxy resin

Colour:				brown / mat

Fields of Application:	  parts of equipment exposed to hot water and vapour

in alkaline environment

Chemical Resistance:		diffusion resistant in aqueous, alkaline to weak acid 	media and vapours

Film Thickness:		           	approx. 250 µm

Temperature Resistance:		- 100º C to + 180 ºC

Heat conductivity:			3,12 W/mK

pH-Range:				4 to 13

Pinhole Testing:			800 Volt DC

Pendulum Hardness acc.

to König:				120 sec.

Break-off Resistance:			2 N/mm²

ASTM D 4541

Impact Strength:			530 mm fall / 1 kg

acc. to DIN 55669

  - Processing guidelines for catalytically hardening materials

SÄKAPHEN coating

HR 60 extra G

Construction references

All seams must be through-welded - interrupted welding seams are not permissible. The welding seams must be smooth, all splashes must be removed. Increases and sharp edges must be ground down until they are smooth – radius approx. 3 mm. More rules in accordance with DIN 28051 and 28053.

Surface preparation

The surface must be cleaned to remove oil, fat and other impurities. Metal surfaces are to be blasted SA 3 with a surface roughness of 40 - 60 µm; surface sludge has to be removed by sandblasting or mechanical grinding. Residues have to be blown off (according to Swedish standard 05 59 00 or DIN 4768).

Materials requirements

Theoretical materials requirements are about 1.2 kg/m² with 500µm dry film coating thickness. The recommended dry coating weight is min. 400 - 500 µm.

Mixing

Mixing proportion:	 Component A (material) of 	77 proportion of weight

Component B (hardener) of 	23 proportion of weight

The two components are supplied according to the indicated mixing proportions.

Resin and hardener are to be stirred up separately. Then the hardener is added to the resin and carefully mixed in. Before use the mixture must rest for a short time. Only the prescribed diluter may be used. It is added to the two components after mixing.

The quantity of diluter depends on the temperature, air humidity, the spraying equipment and the desired layer thickness. We recommend adding a max. of 10 %.

The mixture should be processed within 2 ½ hours. Thickened mixtures may not be made processable again by further additives.

Processing temperature

The necessary minimum temperature is +15 °C.

Each layer should be applied after 8 to 24 hours.

Drying times

dust-dry 		90 min.

(+20 °C, 60 % relative humidity)	non-sticking 		  8 h

dry			48 h

overcoatable		8 - 24 h

completely hardened 	7 - 10 days

Painting and rolling

After the addition of max. 10 % HR 60 extra G-diluter the material can be applied by painting or rolling, where a waiting period between 8 and 24 hours (depending on temperature) between the individual layers must be observed. If this period is exceeded, the last layer is to be slightly roughened up. We recommend a total coating thickness of 500 µm, which has to be applied in 4 to 5 single layers.

Conventional spraying

After addition of max. 10 % HR 60 extra G-diluter and adjusting the viscosity to 50 – 60 seconds, according to DIN 53 211 (DIN cup 4), the material is applied with a spray gun, round nozzle diameter 5 mm, pressure approx. 5 bar. Between the individual layers, a waiting period of 8 to 24 hours must be observed (depending on temperature). If this period is exceeded, the last layer has to be roughened up slightly. We recommend applying the total coating thickness of 500 µm in 4 - 5 single layers.

Airless-Spraying

After addition of max. 10 % HR 60 extra G-dilution the material is applied with airless spraying equipment. The minimum performance of the pump must be 8 l/min with a pressure at the nozzle of approx. 200 bar and a nozzle diameter of 0.45-0.53 mm. Waiting period between the individual layers: 8 to 24 hours (depending on temperature). If this period is exceeded, the last layer has to be roughened up slightly. We recommend a total coating thickness of 500µm, which must be applied in 3-4 single layers.

Pore test

Depending on the total coating thickness between 1500 V and 2000 V.

SÄKAPHEN  COATING

H R  60  e x t r a  G

Product Data Sheet

Characteristics:			catalyst cold cured coating, also for repairs of

epoxy-or phenolic resins.

Basis:					two components epoxy-resin

Colour:				red / brilliant,

green / brilliant

Chemical resistance:		resistant to strong alkalines and acids, all type of 	waters, including brackish-, sea- and deionized-water, 	as 	well as inorganic salt solution

Film thickness:			400 up to 500 µm

Temperature resistance:		+ 120° C

Density:				1,10 g/cm3

Coefficient of thermal

expansion:				4 x 10-6 K-1

VDE 0304

Pinhole testing:			max. 2 kV / 500 µm film thickness

Pendulum hardness

acc. to König:				125 sec.

Adhesive strength:			4,0 N/mm²

Tensile strength:			2,0 %

Specific Heat:				1,2 kJ/kg° C

SÄKAPHEN coating

HR 60 extra TG

Construction references

All seams must be through-welded - interrupted welding seams are not permissible. The welding seams must be smooth; all splashes must be removed. Rises and sharp edges must be ground down to smoothness – radius approx. 3 mm. More rules in accordance with DIN 28051 and 28053.

Surface preparation

Adhesion on iron, steel and casting is very good. The surfaces to be coated must be blasted metallic bright (SA 2 ½ to SA 3 according to Swedish standart 055900 or DIN 4768) fat-free, dust-free and dry. For the parts to be coated, the construction notes of DIN 28 053 and 28 051 must be observed.

Structure

1st Layer  		approx. 150 - 170 µ

2nd and 3rd layer 		approx. 75 - 90 µ each

total coating thickness 		approx. 300 - 350 µ

Mixing proportion

The material is to be mixed thoroughly with the hardener in a weight proportion of 86/14. The mixture must rest for a short time before use.

Wet life

After the addition of the hardener the mixture must be processed within 10 – 12 hours. After this period, thickened material must not be diluted and used again.

Processing

SÄKAPHEN HR 60 extra TG may only be processed at temperatures over +10°C. The material can be painted or sprayed undiluted or, if necessary, after addition of a special diluter to adjust the processing viscosity. After pre-hardening of the first layer (approx. 12 hours at 15°C), or after 2 days the latest, the next layer has to be applied. The equipment can be cleaned easily with special diluter after completion of the coating.

Precipitation hardening

The complete structure reaches its full stability after a precipitation hardening time of 8 days at +15°C and may be put under load only after this time. Precipitation hardening can be accelerated by heating 24 hours after the application of the last layer,

at 	60°C for the duration of		4 hours

at 	80°C for the duration of 		2 hours

at	120 °C for the duration of        0.5 hours

The temperature specifications refer to work-piece temperatures.

Productivity

With a layer thickness of approx. 300 µ:

1st layer 		approx.    560 g/m²

2nd and 3rd layer 	approx.    560 g/m²

--------------------------

approx.  1,120 g/m²

Colours 	red / mat, red-brown / mat

Reference

The hardened coating meets the requirements of the "Plastic-Drinking water–recommendations” within the chilled water range. After official examination, the coating is hygienically suitable for painting swimming pools at public baths.

Shelf-life

Coating masses and hardeners can be stored for about 1 year when storing in dry areas and in well-sealed containers.

Safety precautions

During the processing of SÄKAPHEN HR 60 extra TG the usual precautionary measures for solvent-containing coating materials must be observed. Continuous sufficient ventilation of work spaces must be provided. In boilers, tanks and closed areas, fresh air masks must be worn and there must be continuous inflow of fresh air.

Caution

SÄKAPHEN HR 60 extra TG and nitrocellulose lacquers may only be processed in separated areas since nitrocellulose is inflammable.

Other advice

For special cases, experienced colleagues are available in the processing and application technology department. The "technical data sheets" are meant as a customer advisory service and are provided according to our knowledge of the state of technology. They do not relieve of the necessity to examine in each case whether the recommendations given by us lead to the desired success under given circumstances.

SÄKAPHEN Coating

HR 60 extra TG

Product Data Sheet

Coating Type:				two components coating based on modified 							epoxy resin and polyamine curing agent. The 							material should be applied in two or three 							coats to produce the recommended dry film 							thickness

Colour:					red / mat,

red-brown / mat

Fields of Application:			Condensate vessels, desalization plants for 							sea water, deaerators, water boxes of heat 							exchangers, tubes made of steel

Chemical resistance:			resistant to aqueous, weak acid to alkaline 							liquids

Hot water up to 100° C

Diffusion of water vapour

pH Range:					4 – 12

Film thickness:				300 – 350 µm

Temperature Resistance:			- 20° C to + 100° C

Pinhole Testing:				500 Volt / 100 µm dry film thickness

Pendulum hardness

acc. to König:				100 sec.

Adhesive strength:			5 N/mm2

SÄKAPHEN coating

SÄKAFLAKE hybrid 1042/1042S

Construction notes:

All seams must be through-welded - interrupted welding seams are not permissible. Rises and sharp edges must be ground down to smoothness - radius approx. 3 mm. For the constructional design, DIN 28 051 must be observed, for shaping and welding DIN 28 053. Containers must be designed for sufficient intrinsic rigidity that material deformation cannot occur under any circumstances.

SÄKAFLAKE 1042 contains a scale pigment which causes oriented building of numerous barrier layers due to the high degree of filling, which gives an excellent diffusion firmness to the coating. The composition of the formula and its components lead to a synergistic reciprocal effect and to a hybrid formation.

SÄKAFLAKE 1042 consists of 2 components and is available in black-grey.

For a durable corrosion protection, the necessary dry coating weight must be at least

1,0 mm. It can be applied by airless spraying or by area painting and priming in several layers. In this way an extraordinarily high homogeneity of the protective layer is achieved. For airless application, up to 3% special diluter can be mixed in to improve fluidity. For precipitation hardening, ambient temperature is sufficient after the coating process. To accelerate precipitation hardening, a temperature of 60 - 80 ºC over 1 - 2 hours is recommended.

Technical data

Bonding agent basis 		epoxy vinyl ester resin, solved in styrene

Colour 				black-grey

Wet life 			approx. 30 min/ambient temp.

Consumption 			1.8 - 2.2 kg/m² at 1000 µm layer thickness (theoretical)

Mixing proportion 		component A:B 100 : 1.5 weight percent

Density 			~ 1.4 kg/l

Hardness 			80 ± 5 shores D

Ultimate tensile strength	~ 35 N/mm²

Adhesive strength (on steel)	~ 5 N/mm²

Continuous use temperature 	max. 180ºC (depending on the medium)

Steam permeability 		<1 g/m² (20ºC)

Surface preparation

Rust removal by blasting

according to	SIS 055900 and DIN 4768

Purity grade 			SA 2 ½ / SA 3

Roughness depth 		50 - 100 µm

Cleaning after jet

rust removal 	clearing away and/or sucking off and blowing off with dry, oil-free compressed air

Process specifications

Temperatures

- 	Object 			15 - 40 ºC

- 	Area 			15 - 40 ºC

- 	Dew point distance	> 3 K

- 	Coating solution 	10 - 30 ºC

- 	Air humidity 		< 80% relative humidity

Mixing

Stir component A with dissolver disc, add accelerators and mix intensively. It must be made sure that the small quantity of the accelerator is blended with the entire quantity of component A. Then component B is added and mixed again intensively. Avoid air entry (do not stir until it gets bubbly, otherwise strong reduction of the processing time).

Application

Airless spraying equipment	e.g. WIWA 28064 and higher

Approx. operating pressure	250 - 400 bar

Operating pressure at the

spray gun 			160 - 300 bar

Nozzle 			titanium reversal turning 					nozzle 429

High-pressure hose		size 10 mm, size 8 mm size 					6 mm with long tube lengths 					> 40 m, begin with largest 					size.

Area painting/priming 		also in areas with difficult access and for repairs

Wet film thickness per layer 	~ 400 µm

Number of spraying cycles 	2 - 4 up to the necessary 					layer thickness

Dry film thickness 		1,0 mm – 2,0 mm

Drying time between the

spraying courses (layers) 	min. 8 hours/20ºC

SÄKAPHEN Coating

SÄKAFLAKE hybrid 1042

Product Data Sheet

Basis:					two components catalyst cured Hybrid-coating

with glass flakes

Colour:				black-grey

Fields of Application:			storing tanks, container, flue gas drains, reaction

tanks, washing towers, gas cleaning plants

Special Field:				all devices, where a coating with high diffusion

resistance is required

Chemical Resistance:			resistant against weak alkaline up to strong acid 						medias, all type of waters, flue gases as well

as inorganic salt solutions

Film Thickness:			1,0 - 2,0 mm depending on kind of straining

Temperature Resistance:		up to 180º C

pH - Range:				0,5 up to 9; at random recommending as well as

examination of the conditions by manufacturer

Adhesive Strength:			5 N/mm²

Hardness:				80 Shore D + 5 DIN 53505

Tensile Strength:			35 N/mm² DIN EN ISO 527-1 to 3

Elongation:				~ 0,8 % DIN EN ISO 527-1 to 3

Flexural Principal Mode:		50 N/mm²

Water Vapour Permeability: 		 < 1 g/m².d at 20° C DIN 53122-1

Water Absorption:			 < 1,0 %

SÄKAPHEN Coating

SÄKAFLAKE hybrid 1042 S

Product Data Sheet

Basis:					 two components catalyst cured Hybrid-coating

with glass flakes

Colour:				 black - grey

Fields of Application:			 storing tanks, container, flue gas drains, reaction

tanks, washing towers, gas cleaning plants

Special Field:				 all devices, where a coating with electrostatic derivation is 					 required

Chemical Resistance:	resistant against alkaline up to strong acid media, all type of waters, flue gases as well as inorganic salt solutions

Film Thickness:			 1,0 - 2,0 mm depending on kind of straining

Temperature Resistance:		 180 to  200 °C

pH - Range:	0,5 up to 9; in individual cases according to agreement and after consideration of conditions

Adhesive Strength:			  5 N/mm² DIN EN ISO 527-1 up to 3

Hardness:				  70 Shore D + 5 DIN 53505

Tensile Strength:			  25 N/mm2 DIN 53455

Elongation:				  0,8 %

Flexural Principal Mode:		 30 N/mm²

Water Vapour Permeability: 		 < 1 g/m².d at 20° C DIN 53122-1

Water Absorption:			 < 1,0 %

SÄKAPHEN coating

SÄKALINE SG

Construction notes:

All seams must be through-welded - interrupted welding seams are not permissible. Rises and sharp edges must be ground to smoothness - radius approx. 3 mm. For the constructional design, DIN 28 051 must be observed for shaping, DIN 28053 for welding. Containers must be designed for sufficient intrinsic rigidity that material deformation cannot occur under any circumstances.

Surface preparation

The inner walls of the containers are to be pre-treated by blasting according to achieve purity grade SA 2 ½ / SA 3. Welded joints must be free from glow skin and oxide layers. Sharp burrs, notches and splashes must be removed by grinding. Hardness and grain size of the blast grain have to be selected in such a way that a roughness depth of approx. 50µm is achieved.

Material consumption

Depending on the structure of the objects, the surface roughness and the application conditions, the material consumption amounts to

1.5 kg/m² for a dry coating thickness of 1000µm

Dilution

SÄKALINE (components A + B) should be diluted as little as possible when processed through airless spraying. Only a maximum of 2 weight percents of diluter is permitted.

Mixing

Mixing proportion:  	Component A (material) 	100 parts by weight

Component B (hardener) 	14.5 parts by weight

The two components are supplied according to the indicated mixing proportion.

First, component A is stirred with an electrical agitator. It must be ensured that the material

at the tank bottom is stirred up as well. During further agitating, component B is added.

Wet life:

The pot life for a 25-kg bundle of ready material is approx. 30 min at a temperature of +20 °C.

Processing:

The object and material temperature should be at least +15 °C. A surface and ambient temperature of 20 °C are the best conditions. It must be made absolutely certain that the surface temperature is at least 5°C above the dew point, in order to avoid humidity on the surface.

Spots that are difficult access must be painted with a ring- or a area-brush prior to the initial spraying cycle. For better processing and achievement of a layer thickness of approx. 400 µm in the painting procedure, one weight percent of thixotropic agent can be added.

To achieve a dry coating thickness of at least 700 µ, 2-3 layers must be applied. The next layer can be applied after 2-3 hours. The waiting time of 24 hours between the individual layers should not be exceeded.

Drying time

For precipitation hardening, the coating must be interlaced at 90-120°C for 2-3 hours (heating furnace or warm air blower).

Technical specifications for airless spraying

Airless spraying equipment		WiWa 18060 and higher

Approx. operating pressure: 		250-400 bar

Additional equipment:

Airless spray gun 			WiWa

with extension 				1.500 mm

material flow heaters 			WiWa 3,500 - R - (not absolutely 							necessary) Temperature 30 - 40 °C

Material hose 				3/8"

Nozzle: 				Titanium reversal turning nozzle 							427/429

Safety measures

Take care of good ventilation during the coating work. During processing, the relevant rules for the prevention of accidents issued by the respective professional body and regulations for fire and explosion prevention must be observed, as well as health protection regulations.

Most importantly, the data noted on the respective bundles must be observed according to regulations for dangerous materials.

Care must be taken that not even the smallest quantities of the coating material can get into drains.

The data given in the technical instruction card were established in the laboratory and in practice as approximate values. They reflect today's state of the art. Environmental influences, materials and application techniques are beyond our influence. The usability of the material must therefore be examined before use, under realistic conditions.

This advice reflects our best knowledge, however without obligation.

SÄKAPHEN Coating

SÄKALINE SG

Product Data Sheet

Basis:					two components epoxy resin,

highly filled with glass flakes,

solvent free

Colour:				white, redbrown

Fields of Application:			Storage tanks, pipework, filter-

plates, washing towers, water tanks,

suitable for aqueous foodstuff

and potable water up to 90 °C

Characteristics:			high diffusion- and shock-resistance

Excellent resistance to corrosion and abrasion

Film Thickness:			1,0 – 2,0 mm depending on the used medium

Temperature Resistance:	in case of water temperatures till 100° C and temperature drop to sustrate.

Temperature difference = 80° C

ph Range:				1 to 14

Pendulum Hardness

acc. to König:				140 sec.

Adhesive Strength:			3,5 N/mm2

Impact Strength:			560 mm fall / 1 kg

DIN 55669

SÄKAPHEN Coating Material HR 60 extra RE Instruction for Repair SÄKAPHEN HR 60 RE is a repair material for small damages in SÄKAPHEN coatings, BUT cannot be used for coating of big surfaces. HR 60 extra RE is consisting of two components. Before application the thick-pasty basic component (85 g) has to be mixed with the hardener (15 g). In general the small-packages are corresponding to the proportion of mixture mentioned-before. Execution of Repair 1. Remove all contaminations and moisture from the damaged surface, and, if necessary, degrease this with trichloroethylene, benzene or cleaning emulsion. 2. Remove all traces of rust from the metal surface with abrasive paper, and roughen the SÄKAPHEN coating approx. 1 cm around the damage. 3. Secure the roughened surface against non-roughened SÄKAPHEN coating by using adhesive tapes to make sure that the repair material will only be applied to the damaged area and the roughened surface. 4. Mix carefully one unit of HR 60 extra RE basic component with one unit HR 60 extra RE hardener. CAUTION: THIS HARDENER IS IRRITATING THE MUCOUS MEMBRANES, AND, IN CONCENTRATED FORM, HAS A CORROSIVE ACTION ON THE SKIN. This mixture can be used for duration of about 30 minutes (at 20 °C), and should not be diluted. The cleaning agent is only serving for washing the brushes etc. - The mixture should be applied – without delay - in a thick layer with a brush on to the prepared surface. Avoid inclusions of air, because in this case a covering of the damaged area cannot be assured. A final film thickness of about 500 µm should be achieved. The application of two or three layers is recommended. The previous layer should be repainted, when a distributing by the brush is no more possible (after 6 to 8 hours).

- - 2 - - At least 5 days are necessary for hardening the material at a temperature of 20° C. In case that the object must be immediately taken in operation again, we recommend to heat the surrounding area of the repairing with a temperature of 50° to 60° C for duration of 5 hours. This procedure should be carried out not before 6 hours after having applied the material. After finalizing this thermal treatment (duration approx. 5 hours) the repaired area can be stressed. 7. The temperature of the object as well as the temperature during the application should not be less than +15 °C. 8. The repaired areas must show a smooth surface without any blisters or pinholes. The storage life of the unmixed components is at least 6 months at a temperature of 20° C. Storing at lower temperatures can cause crystallization to be dissolved by carefully heating in a water bath of max. 50° C. Before mixing the two components, these must be cooled down to normal temperature. If not, the result is an extremely fast curing reaction before application of the material. Before placing an order we ask you to let us know the type of SÄKAPHEN coating to be repaired. The theoretical consumption is approx. 1 kg/m², but caused by discontinuous application this consumption can be three to four times more. The relative short potlife of the material is the reason for an early hardening.

- SÄKAPHEN Coating Material - SÄKAFLAKE RE - Instruction for repair SÄKAFLAKE RE is a repair material for small damages in SÄKAFLAKE coatings. SÄKAFLAKE RE is consisting of two components. Before application the thick-pasty basic component (985g) has to be mixed with the hardener (15g). In general the small-packages are corresponding to the proportion of mixture mentioned-before. - Execution of Repair 1. Remove all contaminations and moisture from the damaged surface, and, if necessary degrease this with trichloroethylene, benzene or cleaning emulsion. - Remove all traces of rust from the metal surface with abrasive paper, and roughen the SÄKAFLAKE coating approx. 1 cm around the damage. - Secure the roughened surface against non-roughened SÄKAFLAKE coating by using adhesive tapes to make sure that the repair material will only be applied to the damaged area and the roughened surface. - Mix carefully one unit of SÄKAFLAKE RE basic component with one unit SÄKAFLAKE RE hardener. CAUTION: THIS HARDENER IS IRRITATING THE MUCOUS MEMBRANES, AND, IN CONCENTRATED FORM, HAS A CORROSIVE ACTION ON THE SKIN. This mixture can be used for duration of about 30 minutes (at 20° C), and should not be diluted. The cleaning agent is only serving for washing the brushes etc. 5. The mixture should be applied – without delay – in a thick layer with a brush on to the prepared surface. Avoid inclusions of air, because in this case a covering of the damaged area cannot be assured. A final film thickness of about 1000 µm should be achieved. The application of two layers is recommended. The previous layer should be repainted, when a distributing by the brush is no more possible (after 2 to 3 hours). 6. At least 48 h are necessary for hardening the material at a temperature of 20° C. 7. The temperature of the object as well as the temperature during the application should not be less than +15° C.

8. The repaired areas must show a smooth surface without any blisters or pinholes. The storage life of the unmixed components is at least 9 months at a temperature of 20° C. Before mixing the two components, these must have normal temperature. If not, the result is an extremely fast curing reaction before application of the material. The theoretical consumption is approx. 2 kg/m², but caused by discontinuous application this consumption can be two to three times more. The relative short potlife of the material is the - reason for an early hardening.